## Slide 1
Nb3Sn
SEM Top surface view – EDX composition
PCT – Gap Homogeneity
FIB/SEM-EDX – Not much to say for now
Transport in Field Perp.

## Slide 3
Scanning area

## Slide 4
Nb L
Sn L
Cl L
EDX mapping of impurity

## Slide 5
Δ
Γ/Δ
Comparison SEM-EDX-PCT

## Slide 6
Other impurities

## Slide 7
Homogeneity composition in depth?
2.7 meV instead of 3 meV for Nb3Sn
Nb rich surface---just oxide effect?
Comparison SEM-EDX

## Slide 8
Attempt to do depth profiling
Ag
Nb3Sn
Nb
7 kV electron beam -> Probing size ~ 300-330 nm (= step size for line scan)
NOT CONCLUSIVE -> TEM NEXT

## Slide 9
Transport
Tc is taken at half the jump height
Sheet Resistance (= ρ/thick) = 0.341 x Resistance